# UrbanRoof AI
Detailed Diagnostic Report

Generated using Artificial Intelligence
Inspection + Thermal Report Analysis

# 1. Executive Summary

The inspection revealed high severity issues with dampness, efflorescence, and spalling of paint at various locations, including the hall, bedrooms, and bathrooms. Water ingress or condensation is the root cause of these issues. Additionally, there are minor issues with gaps in tile joints and cracks on external walls. It is recommended to investigate and rectify the water ingress or condensation issues, re-paint affected areas, and re-tile areas with gaps in tile joints. Furthermore, cracks on external walls require investigation and repair.

Overall Condition : The property has several structural and water ingress issues that require immediate attention.

## Priority Actions

Investigate and rectify water ingress or condensation issues

Re-paint affected areas

Re-tile areas with gaps in tile joints

Investigate and repair cracks on external walls

# 2. Property Issue Summary

## Issue Distribution

| Issue | Occurrences |
| --- | --- |
| IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY | 1 |
| IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY ...................................................... 35 | 1 |
| IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM | 1 |
| IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM ........................................... 35 | 1 |
| IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 | 1 |
| IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 36 | 1 |
| IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) | 1 |
| IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) ................................................................................................................ 27 | 1 |
| IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). | 1 |
| IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). 28 | 1 |
| IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) | 1 |
| IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) ....................................................................................................... 29 | 1 |
| IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR). | 1 |
| IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR)....................................................................... 30 | 1 |
| IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). | 1 |
| IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). .......................................................................................... 31 | 1 |
| IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) | 1 |
| IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) ..................................................................................................... 32 | 1 |
| IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) | 1 |
| IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) ............ 33 | 1 |
| IMAGE 8: CRACKS ON EXTERNAL WALL ........................................................................... 34 | 1 |
| IMAGE 8: CRACKS ON EXTERNAL WALL Source: Urbanroof Pvt. Ltd. | 1 |
| IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM | 1 |
| IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM .................................... 34 | 1 |
| Images | 1 |

## Severity Distribution

| Severity | Count |
| --- | --- |
| Critical | 0 |
| High | 13 |
| Medium | 0 |
| Low | 0 |
| Unknown | 6 |

# 3. Area-wise Observations

## CEILING (HALL)

### Observation 1

| Issue | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) |
| --- | --- |
| Description | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and repair the water ingress or condensation issue, and apply a suitable waterproofing coating to the ceiling |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) |

#### Inspection Image

## COMMON BATHROOM

### Observation 1

| Issue | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM |
| --- | --- |
| Description | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM |
| Severity | Low |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM |

#### Inspection Image

## EXTERNAL WALL

### Observation 1

| Issue | IMAGE 8: CRACKS ON EXTERNAL WALL Source: Urbanroof Pvt. Ltd. |
| --- | --- |
| Description | IMAGE 8: CRACKS ON EXTERNAL WALL Source: Urbanroof Pvt. Ltd. |
| Severity | High |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 8: CRACKS ON EXTERNAL WALL Source: Urbanroof Pvt. Ltd. |

#### Inspection Image

### Observation 2

| Issue | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM |
| --- | --- |
| Description | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM |
| Severity | High |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM |

#### Inspection Image

## General

### Observation 1

| Issue | Images |
| --- | --- |
| Description | Images |
| Severity | Low |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | Images |

#### Inspection Image

Image Not Available

### Observation 2

| Issue | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) ................................................................................................................ 27 |
| --- | --- |
| Description | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) ................................................................................................................ 27 |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and rectify the water ingress or condensation issue, and re-paint the ceiling with a water-resistant paint |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) ................................................................................................................ 27 |

#### Inspection Image

### Observation 3

| Issue | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). 28 |
| --- | --- |
| Description | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). 28 |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and rectify the source of dampness, consider applying a waterproofing treatment to the affected area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). 28 |

#### Inspection Image

### Observation 4

| Issue | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) ....................................................................................................... 29 |
| --- | --- |
| Description | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) ....................................................................................................... 29 |
| Severity | High |
| Root Cause | Water ingress through the skirting level |
| Recommendation | Investigate and rectify the water ingress issue |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) ....................................................................................................... 29 |

#### Inspection Image

### Observation 5

| Issue | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR)....................................................................... 30 |
| --- | --- |
| Description | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR)....................................................................... 30 |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and repair the source of dampness and repaint the affected area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR)....................................................................... 30 |

#### Inspection Image

### Observation 6

| Issue | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). .......................................................................................... 31 |
| --- | --- |
| Description | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). .......................................................................................... 31 |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and repair the source of dampness, and re-paint the affected area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). .......................................................................................... 31 |

#### Inspection Image

### Observation 7

| Issue | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) ..................................................................................................... 32 |
| --- | --- |
| Description | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) ..................................................................................................... 32 |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and rectify the source of dampness, and repaint the affected area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) ..................................................................................................... 32 |

#### Inspection Image

### Observation 8

| Issue | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) ............ 33 |
| --- | --- |
| Description | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) ............ 33 |
| Severity | Low |
| Root Cause | Poor workmanship or inadequate tile installation |
| Recommendation | Re-tile the affected area and ensure proper joint sealing |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) ............ 33 |

#### Inspection Image

### Observation 9

| Issue | IMAGE 8: CRACKS ON EXTERNAL WALL ........................................................................... 34 |
| --- | --- |
| Description | IMAGE 8: CRACKS ON EXTERNAL WALL ........................................................................... 34 |
| Severity | High |
| Root Cause | Structural damage or settlement |
| Recommendation | Investigate and repair cracks on external wall |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 8: CRACKS ON EXTERNAL WALL ........................................................................... 34 |

#### Inspection Image

### Observation 10

| Issue | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM .................................... 34 |
| --- | --- |
| Description | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM .................................... 34 |
| Severity | Low |
| Root Cause | Poor workmanship or inadequate tile installation |
| Recommendation | Re-tile the affected area and ensure proper joint spacing and grouting |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM .................................... 34 |

#### Inspection Image

### Observation 11

| Issue | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY ...................................................... 35 |
| --- | --- |
| Description | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY ...................................................... 35 |
| Severity | Low |
| Root Cause | Poor workmanship or inadequate tile installation |
| Recommendation | Re-tile the balcony area to ensure proper joint spacing and sealing |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY ...................................................... 35 |

#### Inspection Image

### Observation 12

| Issue | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM ........................................... 35 |
| --- | --- |
| Description | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM ........................................... 35 |
| Severity | High |
| Root Cause | Structural damage due to external factors |
| Recommendation | Investigate and repair cracks on external wall of master bedroom |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM ........................................... 35 |

#### Inspection Image

### Observation 13

| Issue | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 36 |
| --- | --- |
| Description | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 36 |
| Severity | Medium |
| Root Cause | Water ingress and poor maintenance |
| Recommendation | Inspect and repair terrace surface, seal tile joints in bathroom |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 36 |

#### Inspection Image

## MASTER BEDROOM BATHROOM (1 ST FLOOR)

### Observation 1

| Issue | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) |
| --- | --- |
| Description | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) |
| Severity | Low |
| Root Cause | Poor workmanship or inadequate tile installation |
| Recommendation | Re-tile the affected area and ensure proper joint sealing |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) |

#### Inspection Image

## OPEN BALCONY

### Observation 1

| Issue | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY |
| --- | --- |
| Description | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY |
| Severity | Low |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY |

#### Inspection Image

## SKIRTING AND CEILING-WALL CORNER (BEDROOM)

### Observation 1

| Issue | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). |
| --- | --- |
| Description | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue at the skirting level and wall corner of the bedroom |
| Recommendation | Investigate and rectify the water ingress or condensation issue, and consider applying a waterproofing treatment to the affected area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). |

#### Inspection Image

## SKIRTING LEVEL (MASTER BEDROOM)

### Observation 1

| Issue | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). |
| --- | --- |
| Description | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and repair the skirting level and area near the window in the master bedroom to prevent further dampness and paint spalling. |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). |

#### Inspection Image

## SKIRTING LEVEL (PASSAGE AREA)

### Observation 1

| Issue | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) |
| --- | --- |
| Description | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) |
| Severity | High |
| Root Cause | Waterproofing failure or inadequate drainage |
| Recommendation | Investigate and repair waterproofing system, and ensure proper drainage in the common bathroom passage area |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) |

#### Inspection Image

## SKIRTING LEVEL AND CEILING OF MASTER BEDROOM -2(1 ST

### Observation 1

| Issue | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) |
| --- | --- |
| Description | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and rectify the source of dampness and water ingress, and apply a suitable waterproofing treatment to the affected area. |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) |

#### Inspection Image

## STAIRCASE AREA

### Observation 1

| Issue | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR). |
| --- | --- |
| Description | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR). |
| Severity | Medium |
| Root Cause | Water ingress or condensation issue |
| Recommendation | Investigate and repair the dampness and paint spalling issue, and consider upgrading the waterproofing system or improving ventilation in the area. |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR). |

#### Inspection Image

## TERRACE AND MASTER BEDROOM-2 BATHROOM

### Observation 1

| Issue | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 |
| --- | --- |
| Description | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 |
| Severity | Medium |
| Root Cause | Not Available |
| Recommendation | Not Available |
| Similarity Score | Not Matched |
| Matched Observation | Not Available |
| Evidence | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 |

#### Inspection Image

# 4. Severity Assessment

| Severity | Count | Percentage |
| --- | --- | --- |
| Critical | 0 | 0.0% |
| High | 6 | 24.0% |
| Medium | 12 | 48.0% |
| Low | 7 | 28.0% |
| Unknown | 0 | 0.0% |

Several high severity defects were identified. Repair should be prioritized.

# 5. Recommended Actions

## Immediate Actions

Inspect and repair image 11: cracks on external wall of masterberoom in EXTERNAL WALL.

Inspect and repair image 8: cracks on external wall source: urbanroof pvt. ltd. in EXTERNAL WALL.

Investigate and rectify the water ingress issue

Investigate and repair cracks on external wall

Investigate and repair cracks on external wall of master bedroom

Investigate and repair waterproofing system, and ensure proper drainage in the common bathroom passage area

## Planned Maintenance

Inspect and repair image 12: hollowness and vegetation growth observed on terrace surface, gaps observed between tile joints of bathroom in masterbedroom-2 in TERRACE AND MASTER BEDROOM-2 BATHROOM.

Inspect and repair terrace surface, seal tile joints in bathroom

Investigate and rectify the source of dampness and water ingress, and apply a suitable waterproofing treatment to the affected area.

Investigate and rectify the source of dampness, and repaint the affected area

Investigate and rectify the source of dampness, consider applying a waterproofing treatment to the affected area

Investigate and rectify the water ingress or condensation issue, and consider applying a waterproofing treatment to the affected area

Investigate and rectify the water ingress or condensation issue, and re-paint the ceiling with a water-resistant paint

Investigate and repair the dampness and paint spalling issue, and consider upgrading the waterproofing system or improving ventilation in the area.

Investigate and repair the skirting level and area near the window in the master bedroom to prevent further dampness and paint spalling.

Investigate and repair the source of dampness and repaint the affected area

Investigate and repair the source of dampness, and re-paint the affected area

Investigate and repair the water ingress or condensation issue, and apply a suitable waterproofing coating to the ceiling

## Routine Monitoring

Inspect and repair image 10: gaps between tile joints of balcony in OPEN BALCONY.

Inspect and repair image 9: gaps between tile joints of common bathroom in COMMON BATHROOM.

Inspect and repair images in General.

Re-tile the affected area and ensure proper joint sealing

Re-tile the affected area and ensure proper joint spacing and grouting

Re-tile the balcony area to ensure proper joint spacing and sealing

# 6. Additional Notes

Inspection observations were correlated with thermal evidence where available.

Severity has been assigned using rule-based AI analysis.

Recommendations are advisory and should be verified by a qualified structural engineer.

Thermal anomalies do not always indicate structural defects and require engineering judgement.

Total observations analysed : 25

# 7. Missing Information

General: Root cause unavailable.

General: Recommendation unavailable.

EXTERNAL WALL: Root cause unavailable.

EXTERNAL WALL: Recommendation unavailable.

COMMON BATHROOM: Root cause unavailable.

COMMON BATHROOM: Recommendation unavailable.

OPEN BALCONY: Root cause unavailable.

OPEN BALCONY: Recommendation unavailable.

EXTERNAL WALL: Root cause unavailable.

EXTERNAL WALL: Recommendation unavailable.

TERRACE AND MASTER BEDROOM-2 BATHROOM: Root cause unavailable.

TERRACE AND MASTER BEDROOM-2 BATHROOM: Recommendation unavailable.

# 8. Building Health Score

Building Health Score : 0/100

Overall Building Condition : Critical

# 9. Appendix

| ID | Area | Issue | Severity | Matched |
| --- | --- | --- | --- | --- |
| 0 | General | Images | Low | - |
| 1 | General | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) ................................................................................................................ 27 | Medium | - |
| 2 | General | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). 28 | Medium | - |
| 3 | General | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) ....................................................................................................... 29 | High | - |
| 4 | General | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR)....................................................................... 30 | Medium | - |
| 5 | General | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). .......................................................................................... 31 | Medium | - |
| 6 | General | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) ..................................................................................................... 32 | Medium | - |
| 7 | General | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) ............ 33 | Low | - |
| 8 | General | IMAGE 8: CRACKS ON EXTERNAL WALL ........................................................................... 34 | High | - |
| 9 | General | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM .................................... 34 | Low | - |
| 10 | General | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY ...................................................... 35 | Low | - |
| 11 | General | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM ........................................... 35 | High | - |
| 12 | General | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 36 | Medium | - |
| 13 | CEILING (HALL) | IMAGE 1: DAMPNESS, EFFLORESCENCE & SPALLING OF PAINT AT THE CEILING OF HALL (GROUND FLOOR) | Medium | - |
| 14 | SKIRTING AND CEILING-WALL CORNER (BEDROOM) | IMAGE 2: DAMPNESS AT THE SKIRTING LEVEL & WALL CORNER OF BEDROOM (GROUND FLOOR). | Medium | - |
| 15 | SKIRTING LEVEL (PASSAGE AREA) | IMAGE 3: MILD SEEPAGE AT THE SKIRTING LEVEL OF COMMON BATHROOM PASSAGE AREA (GROUND FLOOR) | High | - |
| 16 | STAIRCASE AREA | IMAGE 4: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR THE WINDOW IN MASTER BEDROOM (1 ST FLOOR). | Medium | - |
| 17 | SKIRTING LEVEL (MASTER BEDROOM) | IMAGE 5: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & AREA NEAR WINDOW IN MASTER BEDROOM (1 ST FLOOR). | Medium | - |
| 18 | SKIRTING LEVEL AND CEILING OF MASTER BEDROOM -2(1 ST | IMAGE 6: DAMPNESS & PAINT SPALLING AT SKIRTING LEVEL & CEILING IN MAS TER B EDROOM – 2 (1 ST FLOOR) | Medium | - |
| 19 | MASTER BEDROOM BATHROOM (1 ST FLOOR) | IMAGE 7: GAPS IN TILE JOINTS OF MASTER BEDROOM BATHROOM (1 ST FLOOR) | Low | - |
| 20 | EXTERNAL WALL | IMAGE 8: CRACKS ON EXTERNAL WALL Source: Urbanroof Pvt. Ltd. | High | - |
| 21 | COMMON BATHROOM | IMAGE 9: GAPS BETWEEN TILE JOINTS OF COMMON BATHROOM | Low | - |
| 22 | OPEN BALCONY | IMAGE 10: GAPS BETWEEN TILE JOINTS OF BALCONY | Low | - |
| 23 | EXTERNAL WALL | IMAGE 11: CRACKS ON EXTERNAL WALL OF MASTERBEROOM | High | - |
| 24 | TERRACE AND MASTER BEDROOM-2 BATHROOM | IMAGE 12: HOLLOWNESS AND VEGETATION GROWTH OBSERVED ON TERRACE SURFACE, GAPS OBSERVED BETWEEN TILE JOINTS OF BATHROOM IN MASTERBEDROOM-2 | Medium | - |